## Slide 1
Engineering Lab
EN19003
Metallurgical and Materials Engineering (MME) department

## Slide 2
General introduction to Metallurgical and Materials Engineering
Today’s specific lab experiment: Tensile behavior of different engineering Materials

## Slide 3
Aviation
Structures
Energy storage
Biomaterials
Electronics
Aerospace
Automobiles
Application
of Materials
Why Materials are IMPORTANT

## Slide 4
More niche applications of Materials
Metals/alloys are crucial in Metallurgy and Materials engineering

## Slide 5
Types of materials based on STRUCTURES

## Slide 6: f02_01_pg4
Polycrystal:
high porosity
Polycrystal:
low porosity
Optical: Transmittance
single crystal

## Slide 7: f01_01_pg4
What is Materials Science & Engineering?
What does each of these terms mean?
Science: Investigate the relationships
Engineering: Design or engineer the structure of materials that produce a set of pre-determined properties

## Slide 8: Why Study Materials Engineering?
Design problem involving materials:
Transmission gear, Oil refinery component, Aero-Engine components, Integrated Circuit chips
Select the right material
- Performance in service condition
- Performance over long run
- Cost
Optimization of the properties
Familiarity with the Processing—Structure--Property relationships and the Processing techniques
 Proficient and Confident in judicious selection of materials

## Slide 9
Structure-mechanical property relationships

## Slide 10
Structure-dependent interesting mechanical property
0.14 nm
Graphene is a hexagonal form of ‘Carbon’, the same element which makes ‘Diamond’ and every living being!
Graphene has a Young’s modulus of 1000 GPa, and a tensile strength of 100 GPa. It is 100× STRONGER than STEEL.
It would take an elephant, standing on a pencil to break through a Graphene sheet!!!!!!!!!!!!!!!!!
Graphene
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C

## Slide 11: Structure
: Arrangement of material’s internal components
Subatomic:
Atomic
Microstructure
Macrostructure

## Slide 12
Optical microscope
Strength of materials: defining role of microstructure
1 µm= 10-6 m

## Slide 13
Scanning Electron Microscope
Strength of materials: defining role of microstructure
1 µm= 10-6 m

## Slide 14
High Resolution Transmission Electron Microscope
Individual atoms
Strength of materials: defining role of microstructure
1 nm= 10-9 m

## Slide 15
CCMR
Cryo STEM (Cornell)
Individual vibrating atoms
Science 372.6544 (2021): 826-831
Strength of materials: defining role of microstructure
Video

## Slide 16
Important Material properties for various applications
Hardness
Strength
Modulus
Ductility
Fracture Toughness
Impact toughness
Hardness
Formability
Fatigue resistance
Creep resistance
Electrochemical
Corrosion resistance
Oxidation resistance
Physical
Melting point
Thermal conductivity
Electrical conductivity
Magnetic properties
Transparency
Sonority
Aesthetics
Surface finish
Paint ability
Mechanical

## Slide 17
Important Material properties for various applications
Hardness
Strength
Modulus
Ductility
Fracture Toughness
Impact toughness
Hardness
Weldability
Formability
Wear resistance
Fatigue resistance
Creep resistance
Mechanical
Electrochemical
Corrosion resistance
Oxidation resistance
Physical
Melting point
Thermal conductivity
Electrical conductivity
Magnetic properties
Transparency
Sonority
Aesthetics
Surface finish
Paint ability

## Slide 18
Titanic movie scene
Brittle vs Ductile materials and consequences

## Slide 19
Today’s specific lab experiment:
Tensile behavior of different engineering Materials

## Slide 20: Materials
Testing of ductile material:
  Mild steel
  Copper
Testing of Brittle material:
  Fe-Al alloy

## Slide 21
Mild Steel specimen: Total length= 100 mm, G (l0) = 25 mm, D = 5 mm
Copper specimen: Total length= 100 mm, G = 25 mm, D = 6 mm
Fe-Al alloy flat specimen: L = 100 mm, G = 25 mm, W = 6 mm and T = 3 mm.
Cylindrical Sample geometry
Flat Sample geometry

## Slide 22
Mild Steel Specimen
Copper Specimen
Fe-Al Specimen (Brittle)

## Slide 23
Engineering Stress and Engineering Strain
Engineering Strain:
Ratio of change in length (displacement) to the original length.
e = l/l0 = (l – l0)/l0
Engineering Stress
S = Load/Initial Area = P/A0
Or, P
Or, P
Or, P
Or, P
Guage Portion
Initial cross section area

## Slide 24
Engineering strain, e
Engineering stress, S
Sy
Sf
Su
The engineering stress (S) vs. engineering strain (e) curve for a ductile metal.
eu
ef
0.2 % strain offset
(e=0.002)
Loading and unloading curves showing the recoverable elastic deformation (b, d) and permanent plastic deformation (a, c).
Typical Engineering Stress vs. Engineering Strain curves for a ductile metal

## Slide 25
Engineering Stress-Strain Curve
0.2% Offset Yield Strength, So
Tensile Strength or Ultimate tensile strength, UTS, Su
Uniform Strain, eu
Strain to Fracture, ef
Elastic limit

## Slide 26
Elastic Limit: The point up to which material shows elastic behaviour, i.e., displacement becomes zero as the load is removed. Immediately after elastic limit permanent plastic deformation starts. Elastic limit, however, is extremely difficult to detect as the amount of permanent deformation just after that point is very very small. Therefore, elastic limit is not determined for engineering application.
Some important points on the Stress – Strain curve

## Slide 27
Yield Strength: Point at which small but detectable, or measurable, amount of plastic deformation happens. If yield point phenomenon takes place (like in mild steel specimen) then it becomes easy to identify yield point. If the stress-strain curve is continuous without yield point phenomenon then either 0.1% or 0.2% strain offset method is adopted to locate the yield point (as shown in a schematic above). Stress corresponding to the yield point is yield stress. For structural applications we never want that applied stress exceeds yield strength of the metal as the structure can deform permanently. In contrast, for manufacturing of metal, plastic deformation is required and applied stress has to be higher than the yield strength.
Some important points on the Stress – Strain curve

## Slide 28
Ultimate tensile strength (UTS): It is the maximum engineering stress corresponding to the ‘point of maximum load’. In any case, we do not want the stress to be so high that the maximum load bearing capacity of a metal is exceeded. If that happens then failure becomes inevitable.
Total elongation to failure (ef): Ductility, i.e., deformability of a metal is generally represented by total elongation to failure (in percentage). Ductility is a very important requirement. For an example, If we are drawing a thick rod, to thin wire, then we should be able to perform it without the breaking of the wire.
Uniform elongation to failure (eu): Uniform elongation is a measure of ductility from manufacturing point of view.
When we perform manufacturing, suppose we draw a metal sheet to a beverage can, we do not want necking (i.e., local thinning) to happen during that process, as that becomes a location prone of leakage.

## Slide 29
Reduction in area till fracture (%), .
Toughness: Ability of the material to absorb energy in the plastic range = Area under the stress-strain curve
Important Terminologies

## Slide 30
True Stress, ;
True Strain (, is the change in gauge length at any instant of time, i.e., .
By integration we find, true strain,
.
where, Ai is the minimum cross-sectional area of the gauge at any instant, dl is the change in length over an instant of time when the instantaneous gauge length is li.
True Stress and True Strain

## Slide 31
Relation between stress and strain
l0×A0 = l×A
 A0/A = L/L0
Engineering strain, e = (l-l0)/l0 = l/l0 – 1
 l/l0 = 1+ e
 A0/A = 1+ e
True Stress () = P/A = (P/A0).(A0/A) = S(1+e)
 = S(1+e), is valid up to necking
l0
l
 l
P
P
A0
During plastic deformation, volume remains constant.

## Slide 32
Comparison between engineering stress-strain and true stress-strain curves. (Elastic deformation is very small, and hence, ignored)
Why such a difference?
Follow the next slides

## Slide 33
Question: Why true stress – true strain curve is different from the engineering stress -strain curve?
Answer: A point on true stress - true strain curve lies above and at the left of engineering stress- engineering strain curve. The equations defining true stress, true strain, engineering stress, and engineering strain (as given above) can be referred to understand this aspect. For plastic deformation to happen, stress has to increase continuously to increase the plastic strain and that phenomenon is called ‘strain hardening’. Therefore, true stress inside the specimen increases continuously with the increase in strain at the deforming part of the specimen. However, after a certain amount of uniform deformation, necking happens and the further deformation occurs only within the necked region. The cross-sectional area of the necked region decreases rapidly. As a result, to maintain the increase in true stress, load requirement can decrease. It is to be noted that true stress is the ratio of load and instantaneous cross-section area, which decreases rapidly due to necking. Thus, beyond the point of maximum load (i.e., the UTS point), the engineering stress decreases as it is defined as load divided by a constant (initial cross-sectional area of the specimen). However, after the point of maximum load, a correction needs to be incorporated even in true stress – true strain curve as the specimen shape changes due to necking.

## Slide 34
Question: How a tensile test specimen of ductile material looks like during different stages of plastic deformation?

## Slide 35
Zig-Zag path
Necking accompanied by Void and crack formation

## Slide 36
Question: How to distinguish between a ductile material and a brittle material just by seeing the fractured specimens?
Answer: Ductile material typically undergoes either through ductile rupture or cup-and-cone fracture with dull appearance on fracture surface. In contrast, a brittle material typically shows flat-fracture surface with shiny appearance.
Ductile rupture
Cup and Cone ductile fracture
Flat fracture in brittle material

## Slide 37
Distinct features in fracture surfaces
Cup and Cone Ductile Fracture
Flat and Shiny Brittle Fracture
Metallic Alloys

## Slide 38: Thank You